Gredmann

Production Specification

Product: Bronze Powder

Grade Name: 80/20

- Granulometry

| Mesh | Microns | Spec. |
| --- | --- | --- |
| 100 | >150 |  |
| 200 | >75 | <0.1% |
| 300 | >53 | <5.1% |
| -300 | <53 | >95.0% |

2.Physical Properties

Apparent Density(g/cc)					2.65~3.25

3. Chemical Analysis

Tin(%)									18.50~21.50

Phosphorus(%)						<0.15

Oxygen(%)								<0.15

4.Packing

25kg/drum