Gredmann

Production Specification

Product: Bronze Powder

Grade Name: 67/33

- Granulometry

| Mesh | Microns | Spec. |
| --- | --- | --- |
| 200 | >75 | <0.1% |
| 300 | >53 | <5.0% |
| 350 | >45 |  |
| -350 | <45 |  |

2.Physical Properties

Apparent Density(g/cc)					2.8~3.3

3. Chemical Analysis

Tin(%)									31.0~35.0

Phosphorus(%)						<0.20

Oxygen(%)								<0.15

4.Packing

50kg/drum