Gredmann

PRODUCTION SPECIFICATION

MATERIAL 	: Copper powder

GRADE			: CHM13

Physical Properties:

Purity		: 99.9% min.

Apparent Density	: 1.2 – 1.4 g/cm3

Screen analysis

> 63 um	: 3% max.

>	45 um	: 10% max.

< 	45 um	: 87% min.

Particle distribution:

Averaged size	: 325 mesh

Packing:

50 kg/drum