Gredmann

Production Specification

Product: Copper Powder

Grade Name: GR52

- Granulometry

| Mesh | Microns | Spec. |
| --- | --- | --- |
| 60 | >250 | <5% |
| 100 | >150 | 55%~65% |
| 150 | >106 | Balance |
| -150 | <106 | <2.5% |

2.Physical Properties

Apparent Density(g/cc)					2.7~3.1

3. Chemical Analysis

Copper(%)								>99.0

Oxygen(%)								<0.25